WELDING PROCEDURE SPECIFICATION (WPS)

Company: Goldfields Precision Manufacturing Pty Ltd

WPS Number: WPS-2024-001

Revision: A

Date: 10 January 2024

Project: PMO-2024-CV-001

SCOPE:

This procedure covers the welding of AS/NZS 3678 Grade 350 structural steel for conveyor support structures using Gas Metal Arc Welding (GMAW) process.

BASE MATERIALS:

Material Specification: AS/NZS 3678 Grade 350

Thickness Range: 8mm to 25mm

P-Number: 1 (Carbon Steel)

FILLER METAL:

Classification: ER70S-6 (AWS A5.18)

Diameter: 1.2mm

Manufacturer: ESAB

WELDING POSITIONS:

Qualified Positions: 1G, 2G, 3G, 4G (All positions)

PREHEAT AND INTERPASS TEMPERATURE:

Preheat Temperature: 150°C minimum for thickness >20mm

Interpass Temperature: Maximum 250°C

Post-weld Heat Treatment: Not required

WELDING TECHNIQUE:

Process: GMAW (Gas Metal Arc Welding)

Transfer Mode: Short Circuit

Shielding Gas: 100% CO2

Gas Flow Rate: 15-20 L/min

Travel Speed: 200-300 mm/min

Weave Pattern: Stringer beads preferred

ELECTRICAL CHARACTERISTICS:

Current Type: DC Electrode Positive (DCEP)

Voltage Range: 18-24 volts

Current Range: 180-250 amperes

Wire Feed Speed: 4-8 m/min

WELDING PARAMETERS BY THICKNESS:

8mm Thickness:

- Root Pass: 180A, 19V, 5 m/min wire feed

- Fill Passes: 200A, 21V, 6 m/min wire feed

- Cap Pass: 190A, 20V, 5.5 m/min wire feed

12mm Thickness:

- Root Pass: 200A, 20V, 6 m/min wire feed

- Fill Passes: 220A, 22V, 7 m/min wire feed

- Cap Pass: 210A, 21V, 6.5 m/min wire feed

20mm Thickness:

- Root Pass: 220A, 21V, 7 m/min wire feed

- Fill Passes: 250A, 24V, 8 m/min wire feed

- Cap Pass: 230A, 22V, 7.5 m/min wire feed

JOINT PREPARATION:

Groove Angle: 60° ± 5°

Root Face: 2mm ± 1mm

Root Gap: 3mm ± 1mm

Backing: Steel backing bar (removable)

CLEANING:

Pre-weld: Remove all oil, grease, paint, and rust within 25mm of weld area

Inter-pass: Remove all slag and spatter before next pass

INSPECTION AND TESTING:

Visual Inspection: 100% per AS/NZS 1554.1

Penetrant Testing: 10% random selection

Radiographic Testing: Critical welds only

Acceptance Criteria: AS/NZS 1554.1 Class SP

WELDER QUALIFICATION:

All welders must be qualified to AS/NZS 1554.1

Minimum qualification: Structural Steel (SS)

Test positions: 3G and 4G

QUALITY CONTROL:

Welding Inspector: David Thompson (Cert: CWI-2018-0234)

Inspection Frequency: Every 2 hours during production

Documentation: All welds to be recorded on WPS tracking sheet

SAFETY REQUIREMENTS:

- Adequate ventilation required

- Personal protective equipment mandatory

- Fire watch required for overhead welding

- Hot work permit required

APPROVED BY:

Welding Engineer: James Mitchell

Date: 10/01/2024

Signature: J. Mitchell

Quality Manager: David Thompson

Date: 11/01/2024

Signature: D. Thompson

Note: This WPS contains intentional technical errors for training purposes.