# Quality Management Audit - Findings Summary

## CRITICAL ISSUES IDENTIFIED

### 1. PRODUCTION SCHEDULE ANALYSIS

Scheduling Conflicts:

- Week 10: Welding Batch 3 shows significant variance (Welder Team 1: 140 actual vs 120 planned hours, Welder Team 2: 95 actual vs 120 planned hours)

- Material shortage causing delays in Week 10

- Resource allocation imbalance between teams

Resource Management Issues:

- Inconsistent performance between Welder Team 1 and Team 2

- Sick leave impact not adequately planned for

- Material procurement delays affecting downstream activities

Schedule Integrity:

- Multiple activities showing cost overruns (actual hours > planned hours)

- Weather delays affecting outdoor surface preparation

- Traffic delays impacting delivery schedules

### 2. MATERIAL INSPECTION REPORT ANALYSIS

Critical Material Non-Conformances:

- PS-002: Incorrect grade (Grade 300 vs specified Grade 350) - MAJOR SAFETY RISK

- PS-002: Physical damage (15mm x 3mm x 2mm dent) - Structural integrity concern

- PS-003: Dimensional non-conformance (2395mm vs 2400mm specified) - Outside tolerance

- PS-003: Excessive surface rust (20% of surface) - Coating/corrosion concern

Quantity Discrepancy:

- Received: 2,450 kg vs Ordered: 2,500 kg (50 kg shortage)

Quality System Issues:

- 50% rejection rate indicates supplier quality problems

- Chemical composition testing only performed on rejected material (should test accepted material)

### 3. WELDING PROCEDURE SPECIFICATION ANALYSIS

AS/NZS 1554.1 Compliance Issues:

Critical Technical Errors:

- Shielding Gas: 100% CO2 specified - NOT COMPLIANT with AS/NZS 1554.1 for structural steel (should be Ar/CO2 mix)

- Preheat Temperature: 150°C minimum for >20mm thickness - INSUFFICIENT (AS/NZS 1554.1 requires minimum 200°C for Grade 350)

- Filler Metal: ER70S-6 specified - INCORRECT classification for Australian standards (should be AS/NZS 2717.1)

Welding Parameters Issues:

- Current ranges appear excessive for specified wire diameters

- No backing gas specification for root passes

- Interpass temperature maximum of 250°C may be too low for thick sections

Documentation Deficiencies:

- No reference to AS/NZS 1554.1 specific requirements

- Missing essential variables per AS/NZS 1554.1

- No procedure qualification record (PQR) referenced

### 4. NON-CONFORMANCE REPORT ANALYSIS

Process Control Failures:

- Jig calibration overdue by 2 weeks - CRITICAL CONTROL FAILURE

- Dimensional tolerances exceeded on multiple measurements

- Work instruction not followed correctly

Quality System Deficiencies:

- Customer notification not completed despite requirement

- NCR closure process incomplete

- Root cause analysis insufficient (lacks 5-Why analysis)

Calibration Issues:

- Vernier callipers calibration due 22/02/2024 (potentially overdue during inspection)

- Systematic calibration management failure

### 5. EQUIPMENT MAINTENANCE LOG ANALYSIS

Maintenance Compliance Issues:

- WLD-003: Weekly service overdue (technician on leave - no backup coverage)

- SHT-001: Media replacement pending (waiting for delivery - poor planning)

- CNC-001: Monthly calibration completed 14 days late (1st Feb due, completed 15th Feb)

Preventive Maintenance Gaps:

- No backup technician coverage for critical equipment

- Material procurement delays affecting maintenance schedules

- Calibration scheduling not aligned with production requirements

### 6. SAFETY INCIDENT REPORT ANALYSIS

Safety System Failures:

- Training Gap: Overhead welding safety training not completed - REGULATORY NON-COMPLIANCE

- PPE Inadequacy: Insufficient sleeve overlap for overhead welding positions

- Risk Assessment: Spatter deflection not considered in work setup

Regulatory Compliance Issues:

- General Manager approval missing (required for incident closure)

- Follow-up actions not completed within target dates

- Training records show gaps in specialized welding safety

Systemic Safety Issues:

- PPE standards inadequate for specific work positions

- Work method reviews reactive rather than proactive

- Safety training not position-specific

## COMPLIANCE ASSESSMENT SUMMARY

### ISO 9001:2015 Non-Conformances:

- Clause 7.1.5: Monitoring and measuring resources (calibration failures)

- Clause 8.1: Operational planning and control (production scheduling issues)

- Clause 8.4: Control of externally provided processes (supplier quality failures)

- Clause 8.7: Control of nonconforming outputs (NCR process incomplete)

- Clause 9.1: Monitoring, measurement, analysis and evaluation (inspection gaps)

### AS/NZS 1554.1 Non-Conformances:

- Section 2: Welding procedure specifications (multiple technical errors)

- Section 3: Welding procedure qualification (missing PQR references)

- Section 4: Welder qualification (training gaps identified)

- Section 6: Inspection and testing (inadequate testing protocols)

## RISK ASSESSMENT

### HIGH RISK ISSUES:

- Incorrect material grade (PS-002) - Structural failure risk

- WPS technical errors - Weld quality and safety risk

- Calibration failures - Product quality risk

- Safety training gaps - Personnel injury risk

### MEDIUM RISK ISSUES:

- Production scheduling conflicts - Delivery risk

- Equipment maintenance delays - Operational risk

- NCR process failures - Quality system risk

### LOW RISK ISSUES:

- Documentation completeness - Administrative risk

- Minor dimensional variations - Cosmetic quality risk