MATERIAL INSPECTION REPORT

Company: Goldfields Precision Manufacturing Pty Ltd

Project: PMO-2024-CV-001 - Pilbara Iron Ore Conveyor Components

Report No: MIR-2024-001

Date: 22 January 2024

Inspector: Michael Roberts (Cert. No: QC-2019-045)

MATERIAL DETAILS:

Supplier: Perth Steel Supplies Pty Ltd

Material: AS/NZS 3678 Grade 350 Structural Steel Plate

Purchase Order: PO-2024-0156

Delivery Date: 21 January 2024

Quantity Received: 2,450 kg (ordered: 2,500 kg)

INSPECTION CRITERIA:

- Visual inspection per AS/NZS 3678

- Dimensional verification

- Mill certificate verification

- Surface condition assessment

INSPECTION RESULTS:

Plate ID: PS-001

Dimensions: 2400mm x 1200mm x 12mm (Specified: 2400mm x 1200mm x 12mm) ✓

Surface Condition: Good - minor surface oxidation within acceptable limits ✓

Mill Certificate: Certificate No. MSC-2024-0089 - Grade 350 confirmed ✓

Visual Defects: None observed ✓

Plate ID: PS-002

Dimensions: 2400mm x 1200mm x 12mm (Specified: 2400mm x 1200mm x 12mm) ✓

Surface Condition: Good ✓

Mill Certificate: Certificate No. MSC-2024-0090 - Grade 300 confirmed ✗

Visual Defects: Small dent on edge, 15mm x 3mm x 2mm deep ✗

Plate ID: PS-003

Dimensions: 2395mm x 1200mm x 12mm (Specified: 2400mm x 1200mm x 12mm) ✗

Surface Condition: Excessive rust on 20% of surface ✗

Mill Certificate: Certificate No. MSC-2024-0091 - Grade 350 confirmed ✓

Visual Defects: None observed ✓

Plate ID: PS-004

Dimensions: 2400mm x 1200mm x 12mm (Specified: 2400mm x 1200mm x 12mm) ✓

Surface Condition: Good ✓

Mill Certificate: Certificate No. MSC-2024-0092 - Grade 350 confirmed ✓

Visual Defects: None observed ✓

CHEMICAL COMPOSITION VERIFICATION:

Sample taken from Plate PS-002 for independent testing

Carbon: 0.23% (Max 0.25% per AS/NZS 3678) ✓

Manganese: 1.45% (Max 1.60% per AS/NZS 3678) ✓

Silicon: 0.35% (Max 0.50% per AS/NZS 3678) ✓

Phosphorus: 0.028% (Max 0.035% per AS/NZS 3678) ✓

Sulphur: 0.015% (Max 0.035% per AS/NZS 3678) ✓

MECHANICAL PROPERTIES:

Tensile Strength: 485 MPa (Min 480 MPa per AS/NZS 3678) ✓

Yield Strength: 365 MPa (Min 350 MPa per AS/NZS 3678) ✓

Elongation: 22% (Min 20% per AS/NZS 3678) ✓

DISPOSITION:

PS-001: ACCEPT

PS-002: REJECT - Incorrect grade, physical damage

PS-003: REJECT - Dimensional non-conformance, surface condition

PS-004: ACCEPT

CORRECTIVE ACTION:

1. Contact supplier for replacement of rejected plates

2. Review supplier quality procedures

3. Implement additional incoming inspection checks

Inspector Signature: M. Roberts

Date: 22/01/2024

Quality Manager Approval: D. Thompson

Date: 23/01/2024

Note: This report contains intentional errors for training purposes.